Technical Data Sheet

#939

Reinforced Aluminium Foil Tape

DESCRIPTION:

The unique nature of the reinforced backing gives this product a combination of high tensile strength, flexibility and conformability. The pressure sensitive adhesive system features high long term holding power.

TECHNICAL DATA:

BACKING				         		PE Scrim CLAF/ Aluminium foil

TENSILE STRENGTH				75 N/25mm

ADHESIVE TYPE					Synthetic rubber/resin

ADHESION TO STEEL				18 N/25mm

ELONGATION AT BREAK				20%

TEMPERATURE RANGE				-5°C to 65°C

50 METRE ROLL LENGTHS

STANDARD WIDTHS			NUMBER OF ROLLS PER CARTON

48MM						24

72MM						16

96MM						12

PRECISION PAPER COATINGS PTY LTD	   PH: +61 (02) 97809000  FAX +61(02) 97289966

The detail in this leaflet refers to average test results obtained in our laboratory out of samples chosen from average production.  The results are purely indicative and it is recommended that the user independently ascertain suitability for the application.